Product Data Sheet

MSBC-1000 (For Condensate Return Lines Protection)

MSBC-1000 offers one pack, multi-functional liquid formulation. It is specially designed for the treatment of boiler & condensate lines of industrial steam generation systems. It also offer excellent corrosion protection due to dissolved oxygen in the system

Weak carbonic acid causes severe pitting corrosion in the system, and it usually forms when wet steam or condensate in the steam/condensate lines comes in the contact with CO2 formed in the boiler carry over with steam.

This product shows effective corrosion control properties through its oxygen scavenging and neutralizing nature against free oxygen and carbonic acid in the system

# SPECIFICATIONS

Appearance				:	Clear White to Amber

PH					:	10.0 – 12.0

Solubility in Water			:	Completely miscible

Specific Gravity				:	0.99 to 1.0 at 30 C

APPLICATION AND DOSAGE :

MSBC-1000 should be fed directly in the system. This product can be dosed on the basis of total alkalinity in feed water. Whereas it does not contributes any effect to the TDS level in boiler.

PRECAUTIONS :

MSBC-1000 should not be used in water intended for human consumption.

MSBC-1000 must be handle with proper safety precautions. For open handling,

Person should be equipped with rubber gloves, aprons and goggles. Harmful if swallowed. May cause irritation to skin and eyes. Avoid contact with skin, eyes and clothing. Wash thoroughly after handling. Wash empty drums before dispose off.

# FARST AID :

In case of contact, immediately flush with plenty of water for at least 5 minutes. If swallowed, promptly drink large quantity.

# PACKAGING:

MSBC-1000 is available in 30 Kg packing.